Lecture 4

Hand out HOMEWORK 1: (If HW is due on Tuesdays)

Quantitative description of semiconductor conductivity

We want to understand why the conductivity  (or resistivity ) of a semiconductor varies strongly with T and impurity concentration.

Basic equation	for current density j (A/cm2):

j  =  q N v			q = electron charge (1.610–19 C)

N = number of charges / volume

v = velocity (cm/s)

N and v are the things that matter most

1. N: In a semiconductor there are two “kinds” of charge carriers

 e– in the conduction band, density n (cm–3).  Most of these sit at the bottom of the conduction band at energy EC.

We can estimate their concentration from an approximation to the Fermi distribution.  We saw that

f(E)  =  [ exp((E – )/kT)  +  1 ] –1

Here, we let E = EC and (according to conventional notation)  = EF.  Since EC – EF  0.5 eV in Si >> kT  0.025 eV at 300K, we have

exp((E – )/kT)  >> 1

so that

f(EC)    exp(–(EC – EF)/kT)

Thus, 		n    exp(–(EC – EF)/kT)

(A true equality requires the “density of states.”)

 “holes” in the valence band, density p (cm–3)

Holes are empty states in the valence band whose motion represents the collective motion of all the remaining e– in the valence band.  These collective motions act like a single positive charge.

A crude (and inaccurate) model:

An argument similar to that for e– shows that

p    exp(–(EF – EV)/kT)

where EV = the top of the valence band.

A. Intrinsic semiconductors

In an intrinsic semiconductor with no added impurity, every e- promotion leaves behind one hole, so

ni  =  pi

Thus we see that N = ni + pi = 2ni varies exponentially with T.

B. Doped semiconductors

We can artificially vary the number of e– or holes by adding impurities that are rich or deficient in valence e–.

Example: a. In Si, add a Group V element (P, As, Sb) that has 5

valence e– but only needs to form 4 bonds.  The extra e–

stays very loosely bonded to the impurity with a bond

strength of only 0.04 – 0.05 eV.

At 300K, most of these e- are “donated” into the

conduction band.  Let the donor conc. be ND.  Then

EF – EF,i  =  kT ln (ND / ni)		(EF moves up)

b. Add a Group III element (B, Ga, In) that has 3 valence

e- but wants to form 4 bonds.  An acceptor level forms in

the bandgap 0.04 – 0.05 eV above the valence band.

At 300K, these levels easily accept e- out of the valence

band, leaving holes.  Let the acceptor conc. be NA. Then

EF,i – EF  =  kT ln (NA / ni) 		(EF moves down)

In both examples, we use ppb quantities so the overall

band structure of the solid doesn’t change.

It turns out that there is a “Law of Mass Action” governing n and p.

We can see this from our expressions for n and p in intrinsic material:

np    exp(–(EC – EF)/kT) exp(–(EF – EV)/kT)

=  exp(–(EC – EV)/kT)  =  exp(–Eg/kT)	Since EC – EV = Eg

More quantitatively,

np  =  NCNV(–Eg/kT)	where NC = 2.801019 cm-3 is the effective

density of states in the conduction band

NV = 1.041019 cm-3 is the effective

density of states in the valence band

(Both for Si at 300K)

With Eg = 1.11 eV, we get ni = pi = 8.15109 cm-3 at 300K

But the Law of Mass Action holds even when there is doping.  Typical levels are 1014 cm-3 or more, so ND (or NA) >> ni (or pi).  Then

 n-doping:	n = ND  =  NCexp(–(EC – EF)/kT)  and  p = ni2 / ND

 p-doping:	p = NA  =  NVexp(–(EF – EV)/kT)  and  n = ni2 / NA

(These equations help calculate the Fermi Level too.)

A curious phenomenon: n + p varies like a “V” with n

2. v (carrier velocity, cm/s):

In semiconductors, charge carriers move ballistically in well-defined wavefunctions about 0.1 m before scattering off a lattice defect or vibration.  Over larger distances, carriers move like gases.

 No electric field  motion like simple gas diffusion

 Electric field  viscous flow like in a pressure gradient

With a field, we find phenomenologically that:

v  =   E			E  = electric field (V/cm)

 = mobility (cm2/Vs)

In general n  p so that electron and hole velocities differ.

For a small field of 1 V/cm (like a battery), in Si 	n = 1300

p = 500

So 	vn = 1300 cm/s

vp = 500 cm/s		These are small numbers compared with

the wavefunctions, which move at  1%

the speed of light, or 108 cm/s.

3. Putting it all together,

j  =  q N v

=  q n n E  + q p p E   =  E / 

So 		  =  1 / q (n n  +  p p)		This is Ohm’s Law.

 in -cm

Now,  decreases slowly as T rises (increased scattering)

A. Intrinsic semiconductors

But n and p increase exponentially and more than compensate the decrease in .

Thus,  decreases with T while  = 1/ increases.

B. Doped semiconductors

Now n and p remain constant at ND and NA respectively (until ni increases above the larger of ND or NA).  Thus,  and  are about constant.

Lecture End ––––