# Lecture 8

# Wet Etching

# Current uses:		remove damage from whole wafer slices

	delineate crystal defects

	planarization by chemical mechanical polishing

	not for fine features

### Advantages:		little substrate damage

	often highly selective

Disadvantages:		Isotropic (usually)		undercutting

	Difficult to control

	Particle contamination (sometimes)

	Susceptibility to scum poisoning

Isotropic etch				Anisotropic etch (plasma)

See Handout 5 (Fig. 6.3) for general setup

General chemical features

Any step can be rate limiting.  Stirring/agitation can reduce (but not remove diffusion limitation.

### Tests for diffusion limitation:		weak T dependence of rate

	more agitation increases rate

See Handout 5 (Fig. 6.5) for example of rxn/diffusion regimes

Mechanisms:  General Features

-	Often incompletely understood

-	May involve intermediates not given in overall stoichiometry

-	Reported etch rates for a system may differ substantially (factors of >2) because of

- difficulty of measuring surface T for fast exothermic rxn

- bubbling

- sensitivity to contaminants/minor products

- sensitivity to surface defects

Examples:

1.	Si

or CH3COOH,  reduces surface tension  better wetting, smoother surface

Most based on HF – HNO3 – H2O

2 steps:		Si oxidized to SiO2 (natively or by HNO3)

	SiO2 removed by HF

Overall rxn:

18HF + 4HNO3 + 3Si    3H2SiF6 + 4NO(g) + 8H2O

↑

soluble

Notes:		intermediate SiO2 not listed!

	like all etching, this is a redox rxn

Si is oxidized to SiF6-2	(0 to +4)

NO3– is reduced to NO	(+5 to +2)

formal oxidation state

Rates often shown on a ternary diagram:  See Handout 5 (Fig. 6.4)

Too little HNO3		Si not oxidized to SiO2

Too little HF		SiO2 not dissolved

Can be either rxn or diffusion limited  See Handout 5 (Fig. 6.5)

Anisotropic etches

	Used for Si micromachines (MEMS)

	Large, electrically isolated devices for high-voltage or radiation-hard applications

Example: 		Si  +  2KOH  +  H2O    K2SiO3  +  2H2

Etches [111] directions slower than others because of double

layer:  See Handout 5 (Fig. 6.6).

On Si(100) wafers, get					instead of

Resistivity effects

Heavy n or p doping increases rate for conventional

HF – HNO3 – CH3COOH solution by factor of ~15.

	Needed for accurate rate predictions

	Can help delineate heavily doped regions for characterization

	Can help make very thin films by etching underlying substrate

2. SiO2

Most based on HF–H2O

Overall rxn: SiO2  +  6HF    H2SiF6  +  2H2O		No change

in formal

oxid. state.

Mechanism :  very complex

Dilute soln :    3HF   F–  +  HF2–  +  2H+

active

not active

Concentrated soln :  also get H3F4– or H4F5– complexes

Solutions often buffered with NH4F.

Lecture End ––––