# Lecture 9

Review of buffers: Intended mainly to keep pH constant in response to adding acids or bases

Employ weak acids & conjugate bases

HA  H+  +  A–

H3O+

Ka  =  H+ A−HA

dissociation constant

Ka is small for a weak acid

Note: pH=−log10H+

e.g., HF, 25C		Ka=7.2x10−4M= H+ F− HF

Ka is large for a strong acid

e.g. HCl:	Ka >> 1

Quantitative analysis

1.  What is H+ in a weak acid solution of formal concentration CA?

HA H++A−  H+ ≈ A−

not = because of H2O dissociation

Also, CA= HA + H+

⇒Ka=H+ A−HA=H+2CA−H+⇒H+2+KaH+−KaCA=0

For weak acid, CA is fairly large, H+ <<CA

  H+2−KaCA=0 

H+=KaCA

2.	Calculate pH change when 100 ml of 0.05M HCl is added to 400 ml of a buffer that is 0.2M in HF and 0.3 M in NH4F

Ka= H+ F− HF= 7.2x10−4M

Starting  pH:   assume	F− CNH4F	= 0.3M

HF CHF	=0.2M

 H+ 0.3M 0.2M= 7.2x10−4M 	 H+	=4.8x10−4M

 pH	=3.32

Ending pH: H++F−→HF

CHF=400(0.2M)+100(0.05M)500=0.170M

Note:  Both decrease due to distribution

CNH4F=400(0.3M)−100(0.05M)500=0.230M

 H+ 0.23M 0.17M= 7.2x10−4M 	 H+	=5.3x10−4M

 pH	=3.27

ΔpH=−0.05

                      Small

In HF / NH4F buffer, however, the purpose is not just to keep pH constand during rxn.  Adding NH4F also affects, HF2− etc.  This is more complex.       See Handout 5

3.	 Metals

Need for removing metallization, leftover metal from silicidation.  Often either acids or bases work.

bubbles

e.g. Al:	2Al+6NaOH		→	2NaAlO3+3H2

2Al+6HCl			→	2AlCl3+3H2

(even H2O would etch Al, except for passivating oxide)

H2+AlOH3

Typical etch is an acid (since base attacks SiO2)

20 parts by vol			CH3COOH

3					HNO3

77					H3PO4

Problems:	-	Metals polycrystalline → ragged edges

-	Remove alloying compounds in Al (e.g. Si)

(leave precipitates behind)

-	Undercutting in multimetal etch with Au or other passive metal on top

See Handout 5:  this is all redox.

don’t change V for 2e–

2Au				2Au++2e−		−1.5 V

2H++2e−		H2				0 V

____________________________________

2Au+2H+		2Au++H2		−1.5 V

doesn’t go, must be (+)

Similar analysis for Al, Cr, Co, Ni gives (+) voltage

 will etch in pure acid.

Lecture End ––––