# Lecture 10

# Plasma Etching

### Uses:		very fine lines

	deep trenches

### Advantages:		can be very anisotropic

	easy to control

Disadvantages:		selectivity lower than wet etch

	mechanism very complicated

	difficult to predict behavior a priori

	more complex equipment

P=10–4 – 10 torr

Fraction ionized ~10–6

Modes of Operation

- Ion milling (relatively uncommon)

- Use inert gas (Ar) at low P (<10–3 torr), high V

- Etching by physical erosion only

- Anisotropic, poor selectivity

- Considerable damage to substrate

- Reactive ion etching (very common)

- Use reactive F or Cl – containing gas at modest P (10–3 – 10–1 torr), modest V (70 – 300V)

- Etching by nonlinear combination of sputtering and rxn

- Fairly anisotropic, decent selectivity (~25)

- Some damage

- Free radical plasma

- Use reactive F or Cl – containing gas at “hi” P (10–1–10 torr), low V (< 70V)

- Etching by free radical rxns

- Usually isotropic (without sidewall passivation), selectivity good, especially to photoresist, relatively low rate

- Little damage

# Gas Selection

For Si, SiO2, Si3N4, many silicides many metals

 F-based etchants CF4, C2F6, SF6

e.g.:		Si + 4F  SiF4(g)

3SiO2 + 4CF3  2CO + 2CO2 + 3SiF4(g)

SiO2 + 2CHF2  2CO + H2 + SiF4(g)

Si3N4 + 12F  3SiF4 + 2N2

Ti + 4F  TiF4(g)

For Al (no volatile fluoride  passivation)

 Cl-based etchants CCl4, BCl3 + Cl2 + CHCl3 + N2, BCl3 + Cl2

e.g.:	Al + 3Cl  AlCl3(g)

Problems:		cold spots  AlCl3 condenses

	expose to H2O  form HCl (corrosion)

Al2O3 (particles)

	residual surface Cl  corrosion of Al

(flush with F species at end)

For photoresist stripping

 O2 – based etchant

Often multiple gases used because:

	some byproducts deposit passivating layers

(e.g., Photoresist scum)  add a little O2

	etchant may react with main substrate but not its surface oxide covering

# A Closer Look at RIE

1.	Physics:	ungrounded plates become negative w.r.t. plasma because e move further per rf cycle and are depleted from gas phase.

Effect more pronounced when floating (or hot) electrode is smaller than grounded one.

#### Voltage makes ions impinge

at near-normal incidence

(although collisions deflect some)

## Plasma Temperature

Normally T in a gas is characterized by a Boltzmann dist. in velocity u:

fu=4πu2m2πkBT3/2exp−mu2/2kBT

In plasmas, there are several distributions:

Ions, e–, neutrals are different, and ions/e– are not Boltzmann!  To get an idea of T, consider a definition based on mean velocity ū:

T=πmu28kB

On this basis,	Tion ~ 400 – 500K

Te- ~ 10,000K (like sun’s surface!)

However, since T is not well defined, standard theories for thermal chemistry don’t apply.

##### Lecture End _____