Lecture 11

Plasma Etching (continued)

Last time we started to examine RIE, and saw how principles of typical thermal chemistry did not apply.  Let’s examine such effects some more.

Example:  Threshold effects in sputtering

Yield = 0 up to Ec

Typically Ec  20eV

Example:  Angular effects in sputtering

Most effective near 60

Scoop atoms out of surface

Glancing incidence does little.

Example:  Cooperative effects:  XeF2/Ar+ on Si

Need both Ar+ and

XeF2 to etch!

Voltage makes most ions impinge at near-normal incidence (although gas collisions deflect some)

2.  Chemistry

Etching occurs from:		 free radicals (minor effect)

		ion-surface reactions (at lover V)

	 ion sputtering (at higher V)

nonlinear interaction 		 ion stimulated surface rxns



e.g.  Cl2 + Ar+ on Si

Rate expressions:	 	very complicated

 	difficult to make predictions

	affected by 	-	gas composition

-	total P

-	rf power

-	surface T

-	electrode voltage

-	loading

-	gas flowrate

-	electrode composition

(We’ll examine the effects of each

of these in a minute)

General (though not universal) form for a given active species i.

Pressure of neutral species i



ri=ki[e–]Pi



e– concentration

More e- give more ions/radicals from neutral i.

However, collision effectiveness of e– varies with P.

At very low P, plasma not self sustaining

At modest P, P  gives more collisions before e– loss  r 

At high P, P  reduces mean free path, no e- don’t pick up enough energy between collisions  r 

Thus

Other process variables:

- rf power  increases make [e–] rise  higher r

- surface T  increasing T often increases r weakly with Arrhenius dependence

- loading (increasing number of wafers)

system-dependent constants

Usually r=k11+k2A

exposed area for etching

This is a common kinetic form for surface reactions of any kind.

	gas flow rate  affects loading constants k1, k2

	electrode material  may be sputtered/redeposited (e.g.  Al)

or yield extra gas products (e.g. SiF4 in

F plasmas over Si or SiO2)

Damage effects – difficult to avoid

- structural defects

- foreign ion implantation

- rough surface (especially when etching only part way through a layer  trenches)

- unwanted residues

Reduce effect by clever choice of

- etchant

- electrode materia/design

- sacrificial layer of oxide

Can also do a subsequent annealing/cleaning step

Always tradeoffs!

Lecture End _____