Lecture 12

Physical Vapor Deposition

No chemical reactions here:  contrasted with chemical vapor deposition

Good for:

- Single-element layers (esp. metals)

- ultra-high purity applications

- non-crystalline layers

Two methods:  evaporation and sputtering

1.	Evaporation

Idea:  raise vapor pressure of source by heating  evaporate (or sublimate) and deposit

Do in vacuum for		cleanliness

	long mean free path

Heating methods:

A.  Resistive:  wrap crucible in wire and pass current

- Simple

- Energy-inefficient		point thermal contacts with wire

	poor efficiency of resistive heating with low resistance

- E-beam heating:

bias source with respect to hot filament

- More complicated

- More efficient

2.	Sputtering:

blast material off a target with ions so it deposits on wafers

Ions come from a biased plasma

Physics of sputtering –

schematic diagram:

Sputtered atoms:	Almost all reflected species are neutrals if electron-phonon coupling is weak, as with metals/noble gases.

	sputtered atoms appear above a threshold of about 20 – 30 eV

	Atoms/clusters come off with energies of 10 – 50eV, which heats surface of wafer or directly enhances surface diffusion

Comparison of evaporation, sputter deposition

Evaporation:			Relatively simple

	Generally poorer step coverage

	Difficult to control rates:  vary exponentially with T

Sputtering:				More complex

	Better step coverage

	Easier to control rates:  vary linearly with plasma power

	Better for making alloys, compound materials for this reason

Problems in PVD

1.	Step coverage

Line-of-sight techniques give poor conformality on sidewalls

Improve by:		Rotating wafers during deposition

	Increasing surface diffusion D = Do exp (–Ediff/kT)

by heating wafers with lamp

2.	Stress in film:  causes wafer bowing or film peeling

Usually caused by deposition at high temperature:

- Thermal expansion mismatch with substrate

- Intrinsic stress from recyrstallization

Compressive stress:  wafer becomes

convex

- Tensile stress:  wafer becomes concave

Lecture End _______