Lecture 14

Chemical Vapor Deposition (CVD)

Chemical reactions take place:  gas-phase “source gases” or “precursors” react with hot wafer surface

Examples:

- Si (amorphous, epitaxial or poly) from SiH4 or Si2H6

- GaAs from (C2H5)Ga and AsH3

- InP from (CH3)3In and PH3

Can take advantage of surface chemistry to get:

- selectivity:  growth on some wafer areas not others

Examples:		Epi-Si on Si (but not SiO2) from SiH2Cl2

	TiSi2 on Si (but not SiO2) from TiCl4, SiH4

	W on Si (but not SiO2) from WF6, H2

- very close stoichometry:  like GaAs is exactly 1:1 regardless of source gas ratio

CVD especially good for:

- semiconductors, insulators

- crystalline layers, especially epitaxial (define)  “vapor phase epitaxy,” VPE (because everything is hot  surface diffusion)

Potential problem:  very hazardous (poisonous, pyrophoric) source gases

Several methods:  depend on pressure, mode of heating, other enhancements

1.	Atmospheric-pressure CVD (APCVD)

Done at atmospheric pressure, sometimes in continuous mode

Schematic:

Good for undemanding applications:  control not great because of large gradients in heat, concentration; takes nontrivial time to start and stop reactor.

2.	Low-pressure CVD (LPCVD)

Done below room temperature, usually 10–3 to 10 torr (lower than 10–3 demands more than mechanical pumps)

- Generally done in batch, with single or multiple wafers

- Since gas diffusivities  1/P, growth rates can be faster than APCVD

- Fewer fluid mechanic effects  better uniformity

A.	Conventional furnace

Schematic:

Hot wall gives more uniform wafer T, fewer convection effects

B. Rapid thermal (RTCVD)

Schematic:  (usually part of a cluster tool)

B.  Single-wafer (Rapid-thermal CVD, or RTCVD)

Schematic:  (usually part of a cluster tool)

- Get kinetic advantages from fast (~100oC/s) heating:  less bulk diffusion

- Cold wall  few particulates, other contamination

3.	Plasma-enhanced CVD (PECVD)

Use plasma to:		predissociate gas precursor (most common) for low-T growth

	get surface resputtering onto sidewalls for better uniformity

Examples:		Si3N4 from SiH4 and (N2 or NH3)

	SiO2 from TEOS (tetraethoxysilane, Si(OC2H5)4)

Problem:  get less control over composition than pure surface chemistry gives  results closer to PVD

# Elementary Steps in CVD

Can be controlled by several factors, any of which can be rate-limiting

Schematic:

A typical rate plot in Arrhenius form (log(r) vs. 1/T)

Since surface rates vary exponentially with T, while gas transport varies much more weakly (polynomial, typically T1/2 to T7/4), at sufficiently high T we always are mass-transport limited.

Next time we’ll look more closely at surface effects first, then later at gas transport.

Lecture End _______