Lecture 15

Chemical Vapor Deposition (continued)

Last time we saw where CVD is used and showed schematically the physical processes that control deposition rates:

Schematic:

Let’s look more closely at surface effects first, then later gas transport.

1.	Surface kinetics

A.	Adsorption

We envision a surface as a regular array of discrete adsorption sites of density n (cm-2)

Typically the maximum (or “saturation”) density nsat is 1014 to  1015 cm–2.  For Si it’s 6 to 7  1014 cm–2, depending on cryst. face.

We can define a coverage θ = n/nsat, with 0 θ≤ 1

In simplest models, rate incident flux f ( pressure P)

 “sticking probability” S (typically a function of )

Thus, ra = Sf = S(θ)P / (2πmkTg)1/2

where:		m	=	molecular mass (g)

k	=	Boltzmann’s constant

Tg	=	gas temperature

In real units,

f (molec/cm2-s) = 3.8161020 [300/Tg  28/M]1/2 P (torr)

## where M = molecular weight (e.g., 28 for N2)

## So dependence on Tg and M is weak

These fluxes are really big:  at room temp, get 1/2 mol/cm2 every second impacting!  We’d all be buried in a couple of minutes except that S becomes very low.  At 10–6 torr, it take about 1 s to saturate a surface with S = 1.

In the simplest models, S = So (1 – θ)N

where usually N	=	1 (first-order, non-dissociative: e.g., H2O on Si)

=	2 (second-order, dissociative:  e.g., H2 on a metal)

Typically So has a weak T dependence (on both Tsurf and Tg)

So how does surface concentration vary with time?  This is a simple problem to illustrate how to use adsorption kinetics

Do mass balance on atoms or molecules:  “control volume” is the surface.

In words,

accumulation = in – out + generation – consumption

Let’s assume for the moment:		no reaction (gen, cons = 0)

	no desorption (out = 0)

Then	accumulation = in

or (for a molecule that doesn’t dissociate):

dn/dt    ra   = Sf   = S(n)P/(2πmkTg)1/2

For dissociation:     dn/dt   =   2ra   =   2Sf

Note: the stoichiometric coefficient often, but not always equals N in S().

Integrate:

dt’  =  t  =  (2πmkTg)1/2/P dn’/S(n’)

Expression gives relation between θ and t.  Note that we get

  Pt     This product of P and t is called the “exposure.”

B.	Desorption

In contrast to adsorption (where bonds form but do not break), desorption rates usually have a strong T dependence.

Usually,	rd = kdnN   =   dexp(–Ed/RT)nN

where   R   =   1.987 cal/mol-K

8.62  10–5 eV/K

Again, N is typically 1 or 2

So how does surface concentration vary with time?

Do mass balance on atoms or molecules:  “control volume” is the surface.

In words,

accumulation = in – out + generation – consumption

Let’s assume for the moment: 		no reaction (gen, cons = 0)

	no adsorption (in = 0)

Then	accumulation = – out

or (for a molecule that doesn’t dissociate):

dn/dt   =  –rd   =   –kdnN

or (using n = nsat θ)	nsatdθ/dt   =  –kdnsatNθN

or		dθ/dt   =  –kd nsatN–1θN

If associative desorption like H2,       dn/dt   =  –2rd

Integrate:

dt’  =  t  =  –1/kdnsatN–1 d’/’N

Gives θ vs. t.

Note:  at steady state,	ra   =  rd	(with suitable stoichiometric

coefficients)

This relation is important for the homework.

C.	Surface reaction

Generally the reaction rate has the form:

rR   =   kR nN   =  νRexp(-ER/RT)nN    (eqn in molec/cm2-s)

## D.	Surface diffusion

Usually the diffusion rate is buried into the surface reaction rate constant.

If reaction is surface-diffusion limited, can’t get a universal closed-form expression for reaction rate constant in two dimensions.

If coverage is low (θ < 0.1 or so) for A + A  A2:

rR   =  kR n2    (eqn in molec/cm2-s)

where

kr   =  2πD/ln1θ

and where the (hopping) diffusion coefficient

D = Do exp(–Ediff/RT)

Lecture End ______