# Lecture 18

# Thermal Oxidation

Dry oxidation		Si(s) + O2 (g)  ®  SiO2 (s)

Wet oxidation		Si(s) + 2H2O(g)  ®  SiO2 (g) + 2H2 (g)

Some processes use O2 and H2O

Used for gate dielectric in MOSFETS and field oxide between devices.

# Simplified Deal-Grove Model

3 possible rate-limiting steps:

- diffusion through gas film

- diffusion through oxide

- reaction at interface

In principle all 3 can contribute.

In Si oxidation, gas diffusion is always very fast compared to the other steps: gas diffusivities are very high.

1.  Diffusion across oxide limits:

Jo2=−Ddcdx ≈−DΔcΔx =−DCo−Cih

## (in molec/cm2-s)

## Linearizes derivative over entire film.  This is an approximation.

Use Henry’s law (dilute solution in solid) to get Co:

Co=khCs=HPo2

­

conventional notation.

This implies diffusion is not so fast to destroy equilibrium at interface.

Jo2=DHPo2−Cih

- Reaction at interface limits:  r (molec/cm2-s) = kCi

Put together:  r=Jo2		⇒	DHPo2−Cih=kCi

to get Ci

⇒	DHPo2−DCi=hkCi

⇒DHPo2=hk+DCi	⇒	Ci=DHPo2hk+D=HPo21+hkD

Thus, r=kHPo21+hkD=N1dhdt

­

molecules O2 /unit vol. SiO2

IC: h(0) = ho

Then solution is:  h2+2Dkh=2DHPo2N1t+τ

τ=ho2+2Dkho2DHPo2N1

Let		A=2Dk			B=2DHPo2N1

Then					τ=ho2+AhoB

Two regimes:

- Linear, 	h→0⇒h≈BAt+τ		Rxn and diffusion matter

- Parabolic, h→∞⇒h≈Bt+τ	Diffusion dominates

Note:  Both A and B have activation energies:

B ∝ exp−EdiffRT

A ∝  exp−(Ediff−ER)RT

Thus, for h ® 0,	EA » ER

h ® ¥, 	EA » Ediff / 2

For very small total thicknesses (<30 nm), Deal-Grove model breaks down:  rate is faster than expected.

Nobody knows why.  Campbell’s book shows a “scotch tape” parameterization of t to make the data fit.

Effects of Dopants:

All dopants increase rate.  Some prefer to segregate into oxide.  Campbell’s Fig. 4-16 misleading – has mass balance problems.

impurity in Si

Define segregation coeff.   m = 	––––––––––––

impurity in SiO2

m < 1 (Segregate to oxide)

m > 1 (Segregate to Si)

Slow diffusion in oxide			Fast diffusion in oxide

Lecture End _________