Lecture 21

Hand out HOMEWORK 5: Explain …

# Heat Transfer in Czochralski Growth

Physical

picture

Assume constant physical properties (not correct), steady state

Full equation in solid:  (differential energy balance)

accum = in – out + gen – cons

ρCp∂T∂t=−ρCpυ⋅∇T+ks∇2T+qgen

0				0

accum.	in-out	   in-out

(flow)	(diffusion)

If we assume radial symmetry, and convective/radiative heat transfer on the circumference, we can integrate out the radial dependence to get

ρCpVdTdx=ksd2Tdx2−2hRT−Ts−2Rqr				(1)

radiative heat flux

Stefan-Boltzmann const.

Now qr has the general form AradεσT4−Ts4

emissivity

where Arad is a complex function of crucible geometry, temperatures, emittances.

Eq (1) needs two BC’s:

melt

1. At x=0, T = Tm

solid–liquid interface

2. At x=L,  −kSdTdx=εσ T4−Ts4+h T−Ts

top end         heat flux

Now, 	 pull velocity V tends to be low

 most cooling is by radiation

There are various approaches to solution.  What we really want is the maximum pull rate Vmax.

This we can get by an energy balance at the interface where solidification takes place:

Diagram:

ΔHmM=−ksdTsdxx=0A−−kLdTLdxx=0A

mass freezing							0 (with

rate, g/s							perfect mixing)

gen	        out into solid	   in from liquid

accum = in – out + gen	 	gen = out – in

Now M=ρsVA		where the cross section area A = R2

	 for max V, get       Vmax=−ksρsΔHmdTsdxx=0

The solution to (1) (on p. 2) gives [dTs/dx]x=0.  If pull any faster than this, the heat of fusion can’t be conducted away into the solid fast enough.

So let’s estimate the maximum pull rate using real numbers:

Let 	dTs/dx  100C/cm			Hm  =  1810 J/g

ks = 0.216 W/cmK			s  =  2.29 g/cm3

⇒Vmax≈0.216 Js⋅cm⋅k2.29 gcm31810 Jg100 Kcm=0.0052 cms

=  0.31 cm/min

The actual pull rate is always lower than the ideal.

Why?	(1)	Usually [dTL/dx]x=0 < 0 instead of = 0, because of cooling of free liquid interface.  This means extra heat is pumped into solid from liquid kLdTLdxA<0, so freezing rate must drop to compensate.

Can fix this by dropping melt interface deeper into crucible so it won’t cool as much, but need to replenish molten Si during growth.

(2)	Fast pulling means fast cooling, and closed loop T control can’t follow fast enough  entire melt starts to freeze.

(3)	Radial T is not uniform.  Coolest on solid surface  strains.

(4)	Impurity (e.g., dopant) pileup at liquid interface decreases melting temp.

If temperature boundary layer extends further into melt then concentration boundary layer, Tm rises faster than T going into melt  unwanted nucleation in melt near interface.

Diagram:

Lecture End ––––