Lecture 22

## Methods for Diffusional Doping

This method is used for noncritical applications because need extended annealing times at high T.  Main doping method for critical applications is ion implantation (which we discuss next lecture)

An experimental method is PGILD (projection gas immersion laser doping)  Idea:

 melt thin surface region with laser

 dopant goes from gas into liquid

 it redistributes evenly (diffusion a factor of 108 faster than in solid)

Idea behind diffusional doping:

 deposit a layer of dopant oxide

 “drive in” dopant at elevated T by solid diffusion

Four oxide deposition methods (Campbell says little about this):

1. Spin-on

Deposit oxide (e.g., B2O3) of

dopant in a slurry and spin

over wafer

vacuum chuck: forms thin layer

Advantages:		 simple

 applies to almost any dopant

Disadvantages:	 poor uniformity (worst of any technique)

Uses: 			 non-critical doping applications where good

control not needed

2. Solid source

quartz, Si poly, or SiC tube

Heat up boat yielding vapor

of dopant oxide (e.g., B2O3,

As2O3, or Sb2O3 in Pt, SiO2, Si, or SiC boat)

Doping level controlled by T

carrier	     source					of source (sublimation

gases 							pressure)

(N2/O2)

Advantage: 		 good for large–area wafers

 can be used when wafers are stacked close

Disadvantage:		 on/off control poorer than for liquid/gas source

because of slow source heating/cooling

3. Liquid source

Like solid source except

bubble carrier gas through T–

controlled liquid (e.g., BBr3,

POCl3: phosphorous

oxychloride)

### Doping level set by vapor pressure of liquid: permit equilibration for control.

Advantages/Disadvantages: 	 like solid source, except on/off control

by valves is faster, better

 ES&H problems: hazardous gases,

halogen disposal

4. Gas source

Like liquid source except need no bubbler: source gases have high vapor pressure.  (e.g., BCl3, B2H6, PH3, AsH3, SbH3)

Add O2 to carrier (like N2) to ensure oxide formation.

Advantages/Disadvantages: 	 like liquid source, except more

pronounced

## Solid Diffusion Physics

Unlike diffusion in liquids/gases, solid diffusion involves breaking chemical bonds, so there is a large T dependence.

Thus, 	D  =  Do exp(–Ediff/kT)

Simplified diffusion mechanisms:

1. “Direct” diffusion by interstitial hopping

Occurs in semiconductors or other solids with an open structure, not metals (which are close packed)

Basically self–  or heteroatoms squeeze between the host atoms on their sites.  The squeezing stretches chemical bonds among the host atoms and yields a barrier.

Examples: H, metals (Fe, Cu, Ni) in Si

Ediff  0.5 – 1 eV

Larger values are for

bigger atoms

2. “Indirect” diffusion mediated by a point defect

Kinds of defects:

A. Substitutional

These atoms are largely

immobile

B. Interstitial

These atoms move

rapidly as we saw above

C. Vacancy

These “holes” can

also move, though

more slowly (since bonds

are broken, not strained)

At 0º K for typical dopants of Groups III and V, interstitial and vacancy defects are unstable with respect to substitutional (since these elements can form 4 bonds)

At higher temperatures, vacancies and interstitials can form with probability :

exp(–Gf,int/kT)			where Gf is the free energy of

formation for the defect

or	exp(–Gf,vac/kT)

These defects eventually equilibrate with the surface (which is a source and sink for interstitials and vacancies)

Vacancies and/or interstitials can also be created or destroyed in nonequilibrium concentrations through various processing steps.

Example: TiSi2 formation requires updiffusion of Si through the silicide, which takes Si from the bulk and injects vacancies into it.

Dopants move in ways mediated by the defects.

A. Vacancy mechanism

Self– or heteroatom moves

by hopping into a neighboring vacancy

Ediff  3.5 – 4 eV

B. Interstitial mechanism

The exact name of mechanism depends on how interstitial atoms are created and destroyed.  Campbell is fuzzy on this point.

1. “Kick-out” or “interstitialcy”

An interstitial atom (host or

foreign) kicks out an

atom on a lattice site.

Ediff  3 eV

2. “Dissociation” or “Frank–Turnbull”

A vacancy forms with creation of

and interstitial, or is annihilated

by an interstitial

Ediff  3.5 – 4 eV

Note: an interstitial can be created by kick-out and destroyed by recombination with a vacancy or vice–versa, although one particular mechanism usually dominates in a given situation.

Lecture End ––––