Lecture 25

Bring and show chips with part of package removed.

# Packaging

This is so-called “back-end” processing.  Describes what happens after wafers are cut up into individual chips called “dice.”

Main purposes of package:

 Provide electrical contact between chip and outside world

 Remove excess heat

 Keep out contamination

Rough process outline:

 Bond back of die to mounting medium

See Handout 7 (Fig. 11-1 and 11.2)

Generally use hard solder (e.g., Au with 2%Si) or a polymer (e.g., Ag-filled epoxy or polyimide).   Need high thermal and electrical conductivity.

 Connect bond pads on circuit side of chip to package leads

See Handout 7 (Fig. 11-5 and 11-4)

Leads are usually Kovar (Fe-Ni-Co alloy).  Several methods exist: “wire bonding,” “tape-automated bonding,” “flip-chip.”  Flip chip is now most common.

 Mold package into final form (& maybe encapsulate/seal)

See Handout 7 (Fig 11-6)

Package body is either plastic (cheap) or ceramic (more expensive but more robust, hermetic sealing).  A new trend: multiple layers of metal in chip and multiple chips in package.  Distinction between chip-level and package-level functions is becoming blurred.

There are many variations on these ideas, most of them proprietary.

Corrosion Issues

Problem:  Electrochemical corrosion (oxidation) of metal leads by environment

Origins:

1. Direct acid attack

e.g.  	Fe + 2H+  Fe+2

Ni + 2H+  Ni+2

Co + 2H+  Co+2

Kovar (Fe-Ni-Co alloy) is a common lead material for ceramic packages.  These rxns solublize the metal.

2. Redox with other metals

e.g.,  		Fe + Pb+2  Fe+2 + Pb

The Pb comes from the low-T glass (PbO / ZnO / B2O3) used to seal a Cerdip package.

3. Stress in package

Metals oxidize more readily under stress.  This is also a problem on metal bridges in winter.

Solution:  Keep out worst contaminators.

A direct O2 attack is not problematic because products are not soluble.

The worst actors are:

1.	H2O		 donates H+ for acid attack.

 provides electrolytic medium, even at monolayer   levels (2-D solution)

 dissolves redox products like NiCl2

2.	Na		Increases ionic strength of electrolyte, providing salt bridge component

Standard electrochemical cell (e.g. Ni)

Inside the package with an inclusion of H2O:

 exchanges readily with other (+) ions on oxide surfaces (ion exchange), so they can do electrochemistry.

3.	Cl		 Salt bridge electrolyte like Na

 Provides counterions for soluble metal redox ions (e.g. FeCl2, NiCl2, etc.) Other counterions (SO4–2) might precipitate.

 In (rare) zero-valent form is a potent oxidizer, e- + Cl  Cl–.  This can happen after plasma processing

Since H2O, Na, and Cl are so ubiquitous, package processes and seals must be very effective at keeping them out.

Steady-State Heat Conduction

# Need to remove heat.  Mechanisms:	  solid conduction

 natural or forced convection

See Handout 7 (Figure 11-9)

Radiation not important (as in Czocholski growth) because T is low, and qr  T4.  Instead,

q = – kT

Conduction     use high thermal conductivity materials for package body, especially in multilayer ceramic (MLC) technology

e.g.,  				Materials				k (W / cm-C)

most common 	Al2O3					0.34

toxic    	BeO					1.84

plastic					0.002 (typical)

(Note:  also need low dielectric constant to avoid RC propagation delays)

Convection	 		At an interface, q = h (T–Tsurr)

	natural:	h lowest

	forced:	h higher, especially for liquids vs. gases

The heat transfer is pretty complicated in general.  A simple configuration is treated in the homework.

Transient Heat Conduction - Thermocycling

Key parameter: expansion coefficient 

For liquids, we usually use coefficient of volume expansion.  This is what you saw in ChE 370.

v = dV/dTV = dlnVdT

For solids, it’s more useful to use coefficient of linear expansion:

v = dL/dTL.

The relation between the two coefficients is:

v = d(L)/dTL=3dL/dTL=3L

Typical value for L:	Metal:      	1.5  10–5 C–1

Ceramic:	0.5  10–6 C–1	(three times smaller)

So expansion L of a given material is given by

L = LLT

e.g. for Ni, L = 13.1  10–6 C–1, 0.2 cm long, 15C thermocycle

L = (13.1  10–6) (0.2) (15) = 3.9  10–5 cm = 0.39 m (small)

The problem is, this exerts huge forces.  Consider the strain E = fractional change in length = L/L, (here 3.9  10–5/0.2  = 2  10–4)

Hooke’s Law:  strain is linear in stress S:  S = E, where  = elastic (or Young’s) modules (This law appears in different form for springs).

For Ni,  = 45  109 N/m2 (units of pressure)

- S = (45  109 N/m2) (2  10–4) = 9  109 N/m2 = 90 atm!

There forces can rupture joints

(When the stress is uniaxial over area A, the force is F = SA)

When stress becomes too high, we get plastic deformation (Hooke’s Law breaks down).

Can also get slow deformation over time (creep)

#### Strain E

Plastic

deformation

# Stress S

In general, the number of cycles a lead can undergo before failing from repeated plastic deformation scales as 1/E2.

Lecture End ––––